《压力容器安全管理工程》教学大纲

一、基本信息

| 课程名称：压力容器安全管理工程 | 英文课程名称：Pressure Vessel Safety Management Engineering |
| --- | --- |
| 课程代码：100306T004 | 总学分： 2 |
| 总学时：32 | 课内学时：32 |
| 实验学时：0 | 上机学时：0 |
| 开课学院：工学院 | 适用专业：过程装备与控制工程 |
| 课程性质：选修 | 先修课程：金工及金属焊接实习、过程装备力学基础、过程设备设计等 |

二、课程简介

压力容器与压力管道的安全运行是世界各国普遍关注和迫切需要解决的重大课题。本课程的教学目的是通过介绍压力容器的失效、安全装置及防脆断安全评定基本分析方法，提高学生分析问题、解决问题的能力，为压力容器及压力管道的安全维护与监察管理打下广泛的基础。

三、教学目标

通过本门课程的学习，学生应达到的总体目标：

目标1：掌握压力容器的基本失效形式与缺陷安全评定的基本方法；

目标2：了解压力容器及压力管道安全监察管理法规，提高对此类特殊设备安全性的认识；

目标3：学生能熟练掌握压力容器的破坏形式和不安全因素，以及防止事故发生的具体措施；

目标4：学生能熟练掌握压力容器缺陷评定的基本原则和方法、压力容器风险分析及预案；

目标5：学生能够了解压力容器的无损检测技术的原理、适用范围及检测程序。

四、教学内容与学习要求

（可按章节顺序或教学单元顺序编写，要详细说明具体教学内容、教学重点和难点，应清楚地表达知识、技能的范围和深度，充分反映课程的知识和技能要求，体现课程特点。）

| 章节/教学单元 |  | 教学内容、重点、难点 | 学时 | 学习要求 |
| --- | --- | --- | --- | --- |
| 第一章 绪论 | 第一节 压力容器安全的重要性 | - 压力容器定义； - 压力容器分类方法； - 压力容器事故及原因。 | 1 | 记忆 应用 |
|  | 第二节 压力容器安全工程的任务 | - 压力容器安全工程的任务； - 压力容器全寿命过程图。 | 0.5 | 记忆 应用 |
|  | 第三节 压力容器安全技术监察与规范 | - 国外压力容器安全技术标准； - 国内压力容器安全技术标准； | 0.5 | 应用 |
| 第二章 压力容器应力分析与安全设计 | 第一节 压力容器应力分析和变形特点 | - 压力容器应力和变形特点； - 压力容器的边缘问题及特性。 | 2 | 理解 应用 综合分析 |
|  | 第二节 压力容器的安全设计 | - 压力容器设计参数的确定； - 压力容器结构的安全设计； - 压力容器用材料的选择； - 压力容器的压力试验。 | 2 | 理解 应用 综合分析 |
| 第三章 压力容器缺陷与破坏形式 | 第一节 压力容器制造缺陷的主要类型 | - 焊接裂纹； - 未焊透和未熔合； - 夹渣； - 气孔； - 表面缺陷； - 组织缺陷。 | 1 | 记忆 应用 综合分析 |
|  | 第二节 压力容器使用过程中产生的缺陷 | - 腐蚀； - 裂纹。 | 0.5 | 记忆 应用 综合分析 |
|  | 第三节 压力容器的破坏形式与预防 | - 延性破裂； - 脆性破裂； - 疲劳破裂 - 腐蚀破裂； - 蠕变破裂。 | 0.5 | 记忆 应用 综合分析 |
| 第四章 压力容器爆破危害与防止 | 第一节 爆炸分类及压力容器爆破的特点 | - 爆炸及其分类； - 压力容器爆炸的特点。 | 1 | 理解 应用 综合分析 |
|  | 第二节 压力容器爆破能量的估算 | - 压缩气体与水蒸气的爆炸能量； - 液化气体与高温饱和水的爆炸能量； - 常温压缩液体的爆炸能量； - 可燃气体器外二次爆炸能量及影响范围； | 2 | 理解 应用 综合分析 |
|  | 第三节 压力容器爆炸的危害。 | - 冲击波的破坏作用； - 碎片的破坏作用； - 爆炸能量与现场破坏能量之间的关系； - 有毒液化气体容器破裂后的毒害区； - 可燃液化气体容器破裂时的燃烧区。 | 1 | 理解 应用 综合分析 |
| 第五章 压力容器超压泄放装置 | 第一节 超压泄放装置与安全泄放量 | - 超压泄放装置的设置原则； - 超压泄放装置的性能； - 压力容器安全泄放量。 | 2 | 记忆 应用 |
|  | 第二节 安全阀的工作原理分类及特点 | - 安全阀的分类； - 安全阀的型号标记； - 安全阀的工作特性； - 额定泄放量的计算； - 安全阀的安装要求及维护。 | 1 | 理解 应用 |
|  | 第三节 爆破片的工作原理分类及特点 | - 爆破片的主要结构形式； - 夹持器； - 爆破片额定泄放面积的计算； - 爆破片的使用和管理。 | 2 | 理解 应用 |
|  | 第四节 爆破片和安全阀的组合使用 | - 爆破片和安全阀的组合使用的特点； - 几种典型组合方法。 | 1 | 理解 应用 |
| 第六章 在用压力容器的安全管理与定期检验 | 第一节 压力容器的使用管理 | - 压力容器的安全使用； - 压力容器的安全管理。 | 0 | 理解 应用 |
|  | 第二节 压力容器的定期检验 | - 检验目的； - 检验要求； - 检验内容； - 合于使用评价； - 基于风险的检验（RBI）； - 检验报告。 | 0 | 理解 应用 |
|  | 第三节 压力容器的常规无损检测 | - 常用的无损检验方法简介； - 压力容器常规无损检验方法比较。 | 0 | 理解 应用 |
| 第七章 压力容器声发射检测及应用 | 第一节 声发射原理及应用概述 | - 声发射及检测原理； - 压力容器声发射检测技术的特点； - 压力容器声发射检测、评估的合理性及难度； - 声发射技术在压力容器结构完整性评价方面的研究进展。 | 0.5 | 记忆 应用 |
|  | 第二节 声发射表征参量与源定位 | - 非统计和统计参量的表征方法； - 声发射源定位。 | 1 | 理解 应用 综合分析 |
|  | 第三节 声发射检测仪器 | - 声发射仪器硬件性能； - 声发射仪器的软件功能。 | 0.5 | 理解 |
|  | 第四节 压力容器声发射检测方法 | - 声发射检测前的准备工作； - 传感器的选择和安装； - 检测仪器的设置和校准； - 压力容器声发射检测过程中的加压程序及控制； - 噪音源的识别与排除； - 数据显示、解释与评价； - 声发射数据的分析与源的分类。 | 1 | 记忆 应用 综合分析 |
|  | 第五节 典型压力容器和常压储罐声发射检测应用实例 | - 大型球罐； - 多层包扎式容器； - 常压立式容器腐蚀状态声发射分析。 | 1 | 应用 综合分析 |
| 第八章 压力容器缺陷安全评定 | 第一节 断裂力学理论基础 | - 断裂力学的形成与发展； - 断裂力学与传统强度理论的差别； - 线弹性断裂力学基本理论； - 弹塑性断裂力学基本理论； - 失效评定图技术及其原理。 | 2 | 理解 应用 综合分析 |
|  | 第二节 在用压力容器缺陷评定方法 | - 缺陷评定中的“合于使用”原则； - 安全监查法规对缺陷评定的基本要求； - 国内外压力容器缺陷评定规范及应用实例。 | 4 | 理解 应用 |
| 第九章 压力容器应急预案与事故分析 | 第一节 事故预防措施与应急准备 | 事故预防措施与应急准备相关内容 | 0.5 | 理解 应用 |
|  | 第二节 应急处理与救援 | 应急处理与救援相关内容 | 0.5 | 理解 应用 |
|  | 第三节 警报解除与事故调查 | 警报解除与事故调查相关内容 | 0.5 | 理解 应用 |
|  | 第四节 压力容器失效分析的目的、意义和要求 | - 失效分析的目的、意义； - 对失效分析人员的要求； - 关于失效分析与损失的几个概念。 | 0.5 | 理解 应用 |
|  | 第五节 压力容器失效形式及原因 | - 断口的宏观分析及宏观特征； - 断口的微观分析及微观特征； - 韧性破裂； - 脆性破裂； - 疲劳破裂； - 腐蚀破裂； - 氢腐蚀； - 腐蚀疲劳； - 蠕变破裂。 | 0.5 | 理解 应用 |
|  | 第六节 压力容器失效分析试验和检测技术 | - 宏观检测； - 无损检测技术； - 理化检验； - 残骸分析； - 断口分析； - 其他。 | 0.5 | 理解 应用 |
|  | 第七节 失效分析方法 | - 特征-因素图法（“鱼骨图”法）； - 事故树分析法。 | 0.5 | 理解 应用 |
|  | 第八节 失效分析主要步骤 | 失效分析主要步骤相关内容 |  | 理解 应用 |
|  | 第九节 压力容器失效分析案例 | 典型案列介绍 | 0.5 | 理解 应用 |
| 合计 |  |  | 32 |  |

注：在“学习要求”一栏补充选项，可以多选，无要求可不填，也可自定要求。记忆，指能从记忆库中找到相关的知识、概念、术语或材料与当前的信息进行比较、确认，能记住并能不加理解的列出、描述这些知识、概念、术语或材料；理解，指能对所学的内容作归纳、分类、解释、总结、推断和一定程度的发挥；应用，指能选择正确的程序应用、实施所学到的内容，并能进行必要的计算或决断；综合分析，指能将所学的内容分解并找出它们的相互关系和构成，或能计划、创造、建造、有改变的重构，或能作评论、总结、估计、预测、评估、论证和答辩。

五、教学方法

本课程在讲授过程中主要以课堂教师讲解为主，在结合大量实际事故范例，强化学生对安全相关基本理论的理解，并培养学生的安全观念；同时辅以相关课外内容的讨论及课堂训练。

六、考核方式

| 是否排考 | 是 |
| --- | --- |
| 考核形式 | 笔试（开卷） |
| 成绩评定方式 | 百分制 |
| 过程成绩/% | 40%（考勤10%+作业20%+研讨10%） |
| 结课考试成绩/% | 60% |

七、教材与参考书

（一）教材

《压力容器安全工程》，第一版，戴光、魏安安等，中国石化出版社，2010年，ISBN：9787511404558。

（二）参考书目或文献

《压力容器安全技术》，第一版，陈凤棉，化学工业出版社，2004年，ISBN：9787502550453。

《压力容器现代设计与安全技术》，第一版，魏新利、吴金星，化学工业出版社，2004年，ISBN：9787502557720。

《化工过程安全——来自事故案例的启示》，第三版，罗伊 E. 桑德斯（段爱军、蓝兴英、姜桂元译），石油工业出版社，2010年，ISBN：9787502175870。

《压力容器安全工程学》,第一版，彭慰华，熊大彬，航空工业出版社，1993，ISBN：7800465705。

|  | 制定人：（课程负责人）王江云 |
| --- | --- |
|  | 审核人：（开课系主任）赵旭亮 |
|  | 制（修）订时间：2024年8月 |

《Pressure Vessel Safety Management Engineering》Syllabus

I. Basic Information

| Course Name: Pressure Vessel Safety Management Engineering | Name in Chinese: 压力容器安全管理工程 |
| --- | --- |
| Course No.: 100306T004 | Total Credits: 2 |
| Total Hours: 32 hour | Lecture Hours: 32 hour |
| Lab Hours: 0 hour | Computer Lab Hours: 0 hour |
| Offering College: College of Engineering | Corresponding Majors: Processing Equipment and Control Engineering, Safety Engineering |
| Course Type：Elective | Prerequisite: Process Equipment Design，Chemical Equipment Design, Metalwork Practice |

II. Course Introduction

It is very important to work safely for pressure vessel and pressure piping, in which caused widespread public concern. The purpose of this course is to provide the basic knowledge about the failure of pressure vessel, the safety device of pressure vessel, and defect assessment methods so on, in order to improve on the capability of solving and analysis problem, leading to construct the base about pressure vessel and pressure piping of security administration and supervise.

III. Course Objective

Through this course, students should be required to attach the following overall objectives:

(1) Master the failure styles of pressure vessel and defect assessment methods.

(2) Understand the codes and standards of pressure vessel and pressure piping.

(3) Master failure styles of pressure vessel and insecurity factor, specific measures to prevent accidents.

(4) Master pressure vessel defect evaluation of the basic principles and methods, pressure vessel risk analysis and plans.

(5) Understand the pressure nondestructive testing technology principle application and test procedures.

IV. Contents and Requirements

Course Content and Requirements for Students' Study

| Chapter/Unit |  | Contents and Key Points | hrs | Requirements |
| --- | --- | --- | --- | --- |
| Part 1: Introduction | Chapter 1: The importance of pressure vessel security | 1. Definition of pressure vessel; 2. Pressure vessel classification method; 3. Pressure vessel accidents and causes. | 1 | Memory Application |
|  | Chapter 2： The mission of pressure vessel safety management engineering | 1. Tasks of pressure vessel safety engineering; 2. The whole life process diagram of pressure vessel. | 0.5 | Memory Application |
|  | Chapter 3： The technical supervision and the standard of pressure vessel safety | 1. Foreign safety technical standards for pressure vessels; 2. Domestic safety technical standards for pressure vessels; | 0.5 | Application |
| Part 2: Pressure vessels stress analysis and safety design | Chapter 1： Pressure vessels stress analysis and deformation characteristics | 1. Stress and deformation characteristics of pressure vessels; 2. Edge problems and characteristics of pressure vessels. | 2 | Comprehension Application Comprehensive Analysis |
|  | Chapter 2： The safety design of the pressure vessel | 1. Determination of pressure vessel design parameters; 2. Safety design of pressure vessel structure; 3. Selection of materials for pressure vessels; 4. Pressure test of pressure vessel. | 2 | Comprehension Application Comprehensive Analysis |
| Part 3: Pressure vessel defects and damage of the form | Chapter 1： The main types of pressure vessel manufacturing defect | 1. Welding cracks; 2. Incomplete penetration and fusion; 3. Slag inclusion; 4. Stomata; 5. Surface defects; 6. Tissue defects. | 1 | Comprehension Application Comprehensive Analysis |
|  | Chapter 2： The process defects of pressure vessel | 1. Corrosion; 2. Crackle. | 0.5 | Comprehension Application Comprehensive Analysis |
|  | Chapter 3: The failure styles of pressure vessel and preventing methods | 1. Ductile rupture; 2. Brittle fracture; 3. Fatigue rupture 4. Corrosion cracking; 5. Creep rupture. | 0.5 | Comprehension Application Comprehensive Analysis |
| Part 4: Pressure vessel blasting damages and prevent | Chapter 1: Explosion classification and pressure blasting characteristics | 1. Explosion and its classification; 2. Characteristics of pressure vessel explosion. | 1 | Comprehension Application Comprehensive Analysis |
|  | Chapter 2: Pressure vessel blasting energy estimate | 1. Explosion energy of compressed gas and water vapor; 2. Explosion energy of liquefied gas and high temperature saturated water; 3. Explosion energy of compressed liquid at room temperature; 4. Energy and influence range of secondary explosion outside combustible gas container; | 2 | Comprehension Application Comprehensive Analysis |
|  | Chapter 3: Pressure vessel explosion hazard | 1. The destructive effect of shock wave; 2. Destruction of debris; 3. The relationship between explosion energy and on-site damage energy; 4. Toxic area after rupture of toxic liquefied gas container; 5. Combustion zone in case of rupture of combustible liquefied gas container. | 1 | Comprehension Application Comprehensive Analysis |
| Part 5: Pressure vessel overpressure bleeder device | Chapter 1: Overpressure bleeder device and safety discharge quantity | 1. Setting principle of overpressure relief device; 2. Performance of overpressure relief device; 3. Safety relief capacity of pressure vessel. | 2 | Memory Comprehension |
|  | Chapter 2: The working principle of safety valve, classification and features | 1. Classification of safety valves; 2. Model mark of safety valve; 3. Operating characteristics of safety valve; 4. Calculation of rated discharge capacity; 5. Installation requirements and maintenance of safety valve. | 1 | Comprehension Application |
|  | Chapter 3： The working principle of rupture disc device, classification and features | 1. Main structural forms of bursting discs; 2. Gripper; 3. Calculation of rated discharge area of bursting disc; 4. Use and management of bursting discs. | 2 | Comprehension Application |
|  | Chapter 4: The combination using of safety valve and rupture disc device | 1. Characteristics of combined use of bursting disc and safety valve; 2. Several typical combination methods. | 1 | Comprehension Application |
| Part 6: pressure vessel in the safety management and regular inspection | Chapter 1: Utilization management of pressure vessel | 1. Safety use of pressure vessels; 2. Safety management of pressure vessels. | 0 | Comprehension Application |
|  | Chapter 2： Regularly inspection of pressure vessel | 1. Inspection purpose; 2. Inspection requirements; 3. Inspection contents; 4. Suitable for use evaluation; 5. Risk Based Inspection (RBI); 6. Inspection report. | 0 | Comprehension Application |
|  | Chapter 3: nondestructive testing of Pressure vessel | 1. Brief introduction of common NDT methods; 2. Comparison of conventional nondestructive testing methods for pressure vessels. | 0 | Comprehension Application |
| Part 7: Pressure vessel acoustic emission test and application | Chapter 1: The principle and application of the acoustic emission | 1. Acoustic emission and detection principle; 2. Characteristics of acoustic emission testing technology for pressure vessels; 3. Rationality and difficulty of acoustic emission detection and evaluation of pressure vessels; 4. Research progress of acoustic emission technology in structural integrity evaluation of pressure vessels. | 0.5 | Comprehension Application |
|  | Chapter 2： Acoustic emission characterization parameter and source orientation | 1. Characterization methods of non statistical and statistical parameters; 2. Acoustic emission source location | 1 | Comprehension Application Comprehensive Analysis |
|  | Chapter 3: Acoustic emission testing instruments | 1. Hardware performance of acoustic emission instrument; 2. Software function of acoustic emission instrument | 0.5 | Comprehension |
|  | Chapter 4: Pressure vessel acoustic emission testing method | 1. Preparations before acoustic emission testing; 2. Selection and installation of sensors; 3. Setting and calibration of testing instruments; 4. Pressurization procedure and control during acoustic emission testing of pressure vessels; 5. Identification and elimination of noise sources; 6. Data display, interpretation and evaluation; 7. Acoustic emission data analysis and source classification. | 1 | Memory Application Comprehensive Analysis |
|  | Chapter 5: Typical pressure vessel and atmospheric pressure tank acoustic emission testing application example | 1. Large spherical tank; 2. Multilayer wrapped container; 3. Acoustic emission analysis of corrosion state of atmospheric vertical vessel. | 1 | Application Comprehensive Analysis |
| Part 8: Pressure vessel defect security evaluation | Chapter 1： Fracture mechanics theory foundation | 1. The formation and development of fracture mechanics; 2. The difference between fracture mechanics and traditional strength theory; 3. Basic theory of linear elastic fracture mechanics; 4. Basic theory of elastic-plastic fracture mechanics; 5. Failure assessment diagram technology and its principle. | 2 | Comprehension Application |
|  | Chapter 2: pressure vessel In use defect evaluation method | 1. The principle of "fit for use" in defect evaluation; 2. Basic requirements for defect assessment in safety supervision regulations; 3．Defect evaluation specifications and application examples of pressure vessels at home and abroad. | 4 | Comprehension Application |
| Part 9: Pressure vessel emergency plan and accident analysis | Chapter 1： Accident prevention measures and emergency preparations | Accident prevention measures and emergency preparedness | 0.5 | Comprehension |
|  | Chapter 2： emergency treatment and rescue | Contents related to emergency treatment and rescue | 0.5 | Comprehension |
|  | Chapter 3: Alarm remove and accident investigation | Alarm cancellation and accident investigation | 0.5 | Comprehension |
|  | Chapter 4: Pressure vessel failure analysis of the aim, significance and requirements | 1. Purpose and significance of failure analysis; 2. Requirements for failure analysts; 3. Some concepts about failure analysis and loss | 0.5 | Comprehension |
|  | Chapter 5： Pressure vessel failure forms and reasons | 1. Macro analysis and macro characteristics of fracture; 2. Micro analysis and micro characteristics of fracture; 3. Ductile fracture; 4. Brittle fracture; 5. Fatigue rupture; 6. Corrosion cracking; 7. Hydrogen corrosion; 8. Corrosion fatigue; 9. Creep rupture. | 0.5 | Comprehension |
|  | Chapter 6: Pressure vessel failure analysis test and inspection technology | 1. Macro inspection; 2. Nondestructive testing technology; 3. Physical and chemical inspection; 4. Debris analysis; 5. Fracture analysis; 6. Other. | 0.5 | Comprehension |
|  | Chapter 7： Failure analysis method | 1. Characteristic factor diagram method ("fishbone diagram" method); 2. Fault tree analysis. | 0.5 | Comprehension |
|  | Chapter 8: Failure analysis main steps | Main steps and related contents of failure analysis |  | Comprehension |
|  | Chapter 9: Pressure vessel failure analysis case | Introduction to typical cases | 0.5 | Comprehension |
| Total |  |  | 32 |  |

Note: in the column of "learning requirements", you can select more than one option. If there is no requirement, you can leave it blank or set your own requirements. Memory refers to the ability to find relevant knowledge, concepts, terms or materials from the memory bank, compare and confirm with the current information, and be able to remember and list and describe these knowledge, concepts, terms or materials without understanding; Comprehension refers to the ability to summarize, classify, explain, summarize, infer and give play to the learned content to a certain extent; Application refers to the ability to select the correct program, apply and implement the learned content, and make necessary calculations or decisions; Comprehensive analysis refers to the ability to decompose the learned content and find out their mutual relationship and composition, or plan, create, build and restructure with changes, or make comments, summaries, estimates, forecasts, evaluations, demonstrations and defense.

V. Teaching Method

This course in the teaching process are mainly composed of classroom teachers explain, in combination with a large number of actual accident examples, strengthen students' understanding of safety related basic theory, and cultivate students' concept of security. At the same time, supplemented by relevant extra-curricular content discussion and classroom training.

VI. Evaluation

| Whether to schedule the test | Yes |
| --- | --- |
| Examination form | Written test (opened) |
| Grade assessment method | Hundred-mark system |
| Process score/% | 50%（attendance10%+homework20%+discussion20%） |
| Final exam results/% | 50% |

VII. Textbook and Reference

(1) Teaching materials

"Pressure Vessel Safety Management Engineering", First edition , Dai Guang, Wei Anan, etc., China Petrochemical Press, 2010, ISBN：9787511404558.

(2) Reference

"Pressure Vessel Safety Technology", First edition, Chen Fengmian, Chemical Industry Press, 2014, ISBN：9787502550453.

"Pressure Vessel Modern Design and Safety Technology", First edition, Wei Xinli, Wu Jinxing, Chemical Industry Press, 2004, ISBN：9787502557720.

"Chemical Process Safety", Third edition, Sanders, R. E., Petroleum Industry Press, 2010, ISBN：9787502175870.

"Pressure Vessel Safety Engineering", First edition, Peng Weihua, Xiong Dabin, Aviation Industry Press, 1993, ISBN：7800465705.